# Part 1 - General

## 1.1      Description

### A. Section Includes preformed metal wall panels, closures, and related trim

## 1.2     Related Sections

### A. 	Division 7 Section - Sheet Metal Flashing and Trim

## 1.3	Submittals

### Shop Drawings by manufacturer only, including the following:

### Product Data

#### Manufacturer’s data sheet including all accessories

### Samples

#### 12” long section of specified panel width and finish

#### 12” long section of continuous cleat

#### Color chart

### Sample Warranties

#### 1. Specified Sample Finish Warranty

## Installer Qualifications

### 5 years experience in the installation of metal wall and soffit systems

## Delivery, Storage, and Handling

### Protect components using best practices to prevent abrasion damage, mechanical abuse, staining discoloration ,or corrosion during manufacturing, shipment and storage.

### Secure panels where they are protected from wind and moisture, while allowing proper drainage and air circulation

### Any unsatisfactory components will be rejected and/or reproduced to meet quality criteria

## Job Conditions

### Coordinate work with related or adjoining trades to prevent damage to stored or installed components

### Verify acceptable storage loads on roof slopes

### Precise location of all roof penetrations shall be verified prior to final roof layout

## Quality Criteria

### A792-96 – Specification for steel sheet, 55% Aluminum-Zinc Alloy coated by the hot-dip process

### E1592-95 – Standard Test Method for Structural Performance of Sheet Metal Roof and Siding Systems by Uniform Static Air Pressure Difference

## Warranties

### Finish/Substrate Warranty – provide manufacturer’s standard form 20 yr finish warranty stating that the finish will not peel, check, crack, chalk, or fade more than 5 E units.

# Part 2 – Products

## 2.1  	Materials

### Galvalume Steel, type AZ-55, grade 50 as per ASTM A792-96

### Gauge: 24 GA (0.024”) or 22 GA (0.030”)

## Metal Wall and Soffit System

### Basis of Design: “Wave” as provided by Architectural Building Components (www.archmetalroof.com) Houston, Texas (800) 423-1105

#### Width: 16”

#### Texture: Smooth

#### Maximum panel length of 40’

### Substitutions shall fully comply with specified requirements in appearance, assembly, and performance

#### Substitutions must be submitted within 10 days of bid date with complete product data

#### No post-bid substitution requests will be considered

## Finishes

### Fluorocarbon Coating: Consists of primer, applied at a nominal dry film thickness of .25 mil and a color coat, applied at a nominal dry film thickness of .75 mil, giving a 1.0 mil nominal dry film on topcoat.  Paint finish should be Kynar 500 as selected from manufacturers standard color selection.  The back side of the material should be .25 mil. Primer and a 0.25 polyester washcoat

## Accessories

### Panel shall be attached to substrate, via continuous clip, at a maximum spacing of 12”

### All fasteners for panel, trim, and structural member attachment will be supplied by metal wall and soffit system manufacturer

### Trim and flashing will be of the same gauge and finish unless approved otherwise by the metal roof system manufacturer.

### D. Sealants and Sealant Tapes will be specified and supplied by the metal    roof system manufacturer

# Part 3 – Execution

## 3.1      Substrate Inspection

### Determine, with the presence of the installer, that structural conditions are satisfactory for panel and trim installation.

### Conflicts resulting from inspection should be resolved prior to soffit/wall panel installation.

## 3.2    	 Panel Installation

### Protective film should be removed prior to extended exposure to sunlight, heat, and other weather elements

### Panels should be handled at seams to prevent buckling

### Consult with adjoining trades to prevent unnecessary damage to the finish

### Install continuous length panels plumb, level, and straight with seams and ribs parallel

### Install panels without excessive waves, warps, or buckles

## 3.3   Panel and Flashing Installation

### All trim shall be installed using the fastener type and spacing in accordance with manufacturer’s instructions

### Fabricate and install sheet metal flashing in accordance with SMACNA manual

### In the process of sheet metal installation, allow no sealant to migrate onto exposed surfaces

### Any damaged product shall be removed and replaced immediately upon recognition

### Touch up paint should be used minimally for minor scratches.  Major scratches or paint failures shall be recognized at damaged and require replacement

### Clean exposed surfaces upon completion of installation to prevent finish damage

# End of Section 07 41 00